## Slide 1: Microwave System
1.5 kW Microwave System
6 kW Solid State Microwave Source

## Slide 2: 2 Potential Heating Methods
  Conductive Heating
  Direct Heating

## Slide 3: Direct Heating
Use microwave energy to heat the material itself
  Just like standard microwave ovens
Very fast!
  Dramatic reactions within seconds
Not applicable to metals
  Reflect MW rather than absorb them (See ElectroBOOM’s video)
Scalability issues
  Localized heating
  Best bulk result after 1.5 hours was a sintered mass

## Slide 4: Conductive Heating
Create crucible that heats due to microwave energy
Slower
  Melting 10-20 grams takes 15-20 minutes
Applicable to almost anything
  The MW energy is absorbed by the crucible material (SiC)
Scalability
  Crucible can scale to heat larger loads
  Larger chambers present new challenges

## Slide 5: Crucibles
Hand-made
  Lower-cost
    We ruin crucibles
    Can make dozens of crucibles for the price of one
  Quick Turn-around
    3 days from idea to reality
  Customization
    Size
    Shape
Silicon Carbide
  Known to heat up due to microwaves

## Slide 6: Final Cavity Design
Target mass: 2kg
  height: 10cm (~3.9”)
  radius: 4.5cm inner (~2.05”)
  thickness: 1.25cm (~0.5”)
Ansys Optimization
  Radius
  Height
  Insulation Thickness
  Waveguide Location

## Slide 7: Final Cavity Design
Goals
  Maximize E-field in crucible
  Minimize S parameter (reflectance)
  Account for manufacturing tolerance/error
Insulation
  Manage high temperatures
  Not heat up from microwaves
  Not create microwave traps
Notes: Ideal radius is 16cm, ideal height is 26.4cm

## Slide 8: Conveyance System
Ease access to the chamber
  Bottom drops out of the cavity
Repurposed 3d printer components
Structure provides framework for microwave leakage safety system
Notes: Controlled with a toggle switch and limit switches

## Slide 9: Current Objectives
Energy efficiency testing
  A key component to the technology’s lunar viability
Preparing simulated Lunar environment
  Lunar environment offers potential benefits
Fabricating final chamber
  Ease of access
  User-friendliness
  Safety features